On the electrical size of metamaterial elements

K. B. Alici1, F. Bilotti2, L. Vegni2, E. Ozbay1

1Nanotechnology Research Center, Department of Physics, Department of Electrical Engineering, Bilkent Universityy

P.O. 06800, Bilkent, Ankara, Turkey

Fax: + 90312–2901015; email: bora@fen.bilkent.edu.tr

2 Department of Applied Electronics, University of Roma Tre Via della Vasca Navale, 84 – 00146, Rome, Italy

As the constituting elements of a negative permeability medium, Pendry proposed electrically small nonmagnetic metallic resonators. [1] By utilizing the available volume more efficiently, we demonstrated that the electrical size of these elements can further be reduced under the restrictions of fabrication techniques. [2, 3] In Fig. 1 we show that the decrease of resonance frequency as the resonator parameters change. These novel µ-negative (MNG) medium elements can be manufactured relatively easy in the domain of well developed printed circuit board manufacturing techniques and optical lithography processes. Since the electrical size of the metamaterial element limits the resolution of the subwavelength imaging, the MNG materials demonstrated here can be the first step towards the metamaterial based ultra-high resolution imaging systems. Moreover, they establish a solution for the antenna miniaturization problem in wireless systems. [4, 5]

Fig.1: Resonance frequency as a function of the number of rings and turns (experiment and simulation).

##### References

[1]    J. B. Pendry, A. J. Holden, D. J. Robbins, W. J. Stewart, “Magnetism from conductors and enhanced nonlinear phenomena,” IEEE Trans. Microwave Theory Tech. 47, 2075 (1999).

[2]   F. Bilotti, A. Toscano, L. Vegni, “Design of Spiral and Multiple Split-Ring Resonators for the Realization of Miniaturized Metamaterial Samples” IEEE Trans. Antennas Propag. 55, 2258 (2007).

[3]   K. B. Alici, F. Bilotti, L. Vegni, E. Ozbay, “Miniaturized negative permeability materials” Appl. Phys. Lett. 91, 071121 (2007).

[4]    K. Buell, H. Mosallaei, K. Sarabandi, “A substrate for small patch antennas providing tunable miniaturization factors,” IEEE Trans. Microwave Theory Tech. 54, 135 (2006).

[5]    K. B. Alici, E. Ozbay, “Electrically small split ring resonator antennas,” J. Appl. Phys. 101, 083104 (2007).